## Slide 1: Reduction of Iron Ore Pellets in a Packed Bed Reactor

## Slide 2: Shrinking Core Model
Packed bed with solid particles
Consumption of reactant particles:
  Solid reactant or solid mixture
  Heterogeneous reactions consume the reactant
  Porous layer forms
x
Unreacted core
Porous layer
Diffusion layer
Bed inlet
Core and layers of a shrinking core particle.

## Slide 3: Shrinking Core Model
Porous layer formed
  Layer grows as the core shrinks:
    Reactions on the core surface consumes the core
    Solid core radius solved for
    Extra dimension for moving coordinate system
    r is a scaled moving system
  Reactants diffuse through the layer
  Volumetric reactions in the porous layer
Core and layers of a shrinking core particle.
r
Rp
Ro
0
1
Reacted layer coordinate:
Core surface position:
Diffusive transport in the reacted layer (extra dimension).
Porous layer
Diffusion layer
Unreacted core

## Slide 4: Iron Ore Pellet Reduction
Ore pellet processes
  Diffusion through porous layer
    CO required for reduction
  Reduction at the FeO surface produces a flux of gas reactants
  FeO core reduced
  Volumetric gas phase reaction in the formed Fe layer
  Reactions rates defined in a Chemistry interface
Porous reacted Fe
Diffusion layer
FeO(s) + CO + s(ads) ⇄ Fe(s) +
Reduction reaction
Surface sites s(ads) indicates a surface reaction. Not used here in the reaction rate.
Gas phase reaction
2 CO + ⇄ 2
Unreacted FeO
(mol/m2s)
(mol/m3s)

## Slide 5: Iron Ore Pellet Reduction
Define reaction kinetics
Add a Packed Bed feature
Enable the Shrinking Core model
Specify core density and composition
Apply the core consuming reaction
Apply the porous layer reaction
Core development
1
2
3
4
5
6

## Slide 6: BED GAS PHASE CONCENTRATION DEVELOPMENT

## Slide 7: PELLET CONCENTRATIONS IN THE MIDDLE OF THE BED

## Slide 8: PELLET CORE RADIUS DEVELOPMENT