## Slide 1: Preconditioning of Surface-Mount Devices (SMDs) for Testing

## Slide 2: OVERVIEW

## Slide 3: Geometry
An insulated-gate bipolar transistor (IGBT) module is studied in this model.
Copper
Die
Sn3Ag
EMC
Ceramics

## Slide 4: Physics and Multiphysics
Physics interfaces
  Solid Mechanics: Thermal expansion
  Transport of Diluted Species: Diffusion coefficient is a function of temperature
Multiphysics couplings
  Hygroscopic Swelling: Hygroscopic Swelling coefficient 0.222 mm3/mg

## Slide 5: Preconditioning Process Steps
Bake
  Removal of moisture in the structure
Moisture soak
  Absorption of moisture in the plastic seal
Reflow
  Reflow of molten solder

## Slide 6: Step 1 – Bake
Duration
  24 h
Temperature
  T1 = 125ºC
  Reference temperature is 25ºC
Moisture conditions
  Initial concentration is 10 mol/m3
    Reference concentration for hydroscopic swelling is 10 mol/m3
  Concentration at outer boundary of plastic seal is set to 0 mol/m3

## Slide 7: Step 2 – Moisture soak
Duration
  192 h
Temperature
  T2 = 40ºC
Moisture conditions
  Initial concentration is 0 mol/m3
    The structure is regarded to be completely dry after baking
  Concentration at outer boundary of plastic seal is kept as 140 mol/m3
    Assuming the moisture is saturated at outer boundary during the step
    The saturation concentration is temperature independent

## Slide 8: Step 3 – Reflow
Duration
  21 min (3 cycles)
Temperature
  Temperature variation T3(t) is defined
    Tmax = 260ºC
    Finally reach room temperature (25ºC)
Moisture conditions
  Initial concentration is taken from the final result of step 2
    Reflow test is conducted immediately after moisture soak
  Concentration at outer boundary of plastic seal is set to 0 mol/m3

## Slide 9: Study
For each process step, includes a transient step and a steady step
  Transient step for moisture diffusion only
  Steady step for structure deformation only: Inherit the concentration results of the transient step by scanning the parameter “t”

## Slide 10: Mesh
Add boundary layer at the outer boundary of the plastic seal to avoid convergence problems caused by concentration discontinuity.

## Slide 11: Materials
Materials | CTE (1/K) | Density (kg/m3) | Young’s modulus (GPa) | Poisson’s ratio
Copper | 17e-6 | 8960 | 110 | 0.35
Die | 2.6e-6 | 2320 | 160 | 0.22
Sn3Ag | 23e-6 | 7440 | 40 | 0.40
EMC | 10e-6 | 1900 | 22 | 0.40
Ceramics | 23e-6 | 2700 | 70 | 0.33

## Slide 12: Results, Bake
Stress distribution after baking step finished

## Slide 13: Results, Bake
Moisture concentration in the plastic seal after baking step finished
With the structure deformation shown.

## Slide 14: Results, Bake
Structure deformation during the baking step

## Slide 15: Results, Moisture Soak
Stress distribution after moisture soak step finished

## Slide 16: Results, Moisture Soak
Moisture concentration in the plastic seal after moisture soak step finished
With the structure deformation shown.

## Slide 17: Results, Moisture Soak
Structure deformation during the moisture soak step

## Slide 18: Results, Reflow
Stress distribution when the temperature peak for the reflow step is reached at t = 6 min

## Slide 19: Results, Reflow
Moisture concentration in the plastic seal when the temperature peak for the reflow step is reached after t = 6 min
With the structure deformation shown.

## Slide 20: Results, Reflow
Structure deformation during the reflow step (3 cycles)

## Slide 21: Summary
Thermal expansion and hygroscopic swelling are considered to mimic the preconditioning test of an IGBT module.
Further extension:
  Heat transfer between structures and surroundings
  More complex constitutive models such as the viscoplasticity for solder materials