## Slide 1: Improving The Design Process Of A MEMS-IR-Emitter Toni Schildhauer, Andreas T. Winzer, Julia Baldauf

## Slide 2: SHORT FACTS – „CiS Forschungsinstitut“
    Research institution in Erfurt, Thuringia, Germany
    Independent - non-profit - close to business
  16,5 MIO. € TOTAL OUTPUT IN 2022
    ~120 Employees
    52 % Public research projects
    48 % Industrial contract research
    and manufacturing
    No basic funding, only project funding
  TECHNOLOGICAL EXPERTISE
  In MEMS and MOEMS sensors
  Simulation
  & Design
  Wafer Technology
  & Manufacturing
  Packaging &
  Assembly
  Test &
  Analytics
→ MOEMS Development
and Prototyping
Notes: Zum mal kurz drüber springen
service provider

## Slide 3: Background: IR-MEMS-Technology And Fabrication

## Slide 4: Background: IR-Emitter-Technology
Rogalski, Antoni & Chrzanowski, K. (2014). Infrared Devices And Techniques (Revision). Metrology and Measurement Systems. 21. 10.2478/mms-2014-0057
(Pulsed) IR-light source
Reference cell
Sample cell
Inlet
Outlet
Detector
with filter
Nondispersive Infrared Gassensor
Notes: Typical Life expectancy: 24h x 365 days x 5 years = 43‘800 h

## Slide 5: Background: IR-Emitter-Technology
+
-
1 mm
1 mm
800 °C
< 150 °C
Ohmic Resistor

## Slide 6: M(O)EMS - Fabrication
Customer query
Design and technology flow
Clean room manufacturing
Wafer inspection and measurements
Assembling
Module testing (performance, life time, …)
Try
Fail
Success = End
Optimization potential
Approval, selling
Process development:
1 month
3-6 month
1 week
2-4 weeks
3-6 month

## Slide 7: M(O)EMS - Fabrication
Customer query
Design and technology flow
Clean room manufacturing
Wafer inspection and measurements
Assembling
Module testing (performance, life time, …)
Try
Fail
Success = End
Optimization potential
Approval, selling
Process development:
1 month
3-6 month
1 week
2-4 weeks
3-6 month

## Slide 8: M(O)EMS - Fabrication
Customer query
Design and technology flow
Clean room manufacturing
Wafer inspection and measurements
Assembling
Module testing (performance, life time, …)
Try
Fail
Success = End
Optimization potential
Approval, telling
Process development:
1 month
3-6 month
1 week
2-4 weeks
3-6 month
SIMULATION
Material Parameters?!
SIMULATION
Improve Design Process
Analyze Current Product

## Slide 9: Building The Model Challenge: Material Parameters Of Our Thin Layers

## Slide 10: The Inverse Problem
forward calculation: obtain the device characteristic
inverse calculation: obtain the material parameters

## Slide 11: The Inverse Problem - Result
630
150
150
°C
°C
Simulation
Heat camera image
630
Chart: Time Scale Comparison

## Slide 12: Using The Model In Design Processes

## Slide 13: First Design Task
Either bright or fast
  Fast
Big discrete parameter studies
  Good prediction, what is worth to manufacture
One lengthwise Beam
One crosswise Beam
Smaller conductive Layer
Two crossed Beams
Current Design
Current Density
Temperature
Radiosity
140
130
120
110
100
90
80
700
600
500
400
300
200
3
2
1
70
0
°C
A/m
W/m²x104

## Slide 14: Helping In Design
Same life time in simulation
Chart: Measurements with fabricated chip
| 1 | 3 | 5 | 7 | 10 | 13 | 15 | 20 | 27 | 35 | 40 | 50 | 80 | 100 | 150 | 180 | 200
Old Design | 1 | 0.99963 | 0.98569 | 0.94936 | 0.85831 | 0.7558 | 0.69371 | 0.56532 | 0.44187 | 0.35085 | 0.31006 | 0.25194 | 0.15825 | 0.12584 | 0.082932 | 0.068324 | 0.060942
New Design | 1.0172 | 1.0119 | 1.0029 | 0.98383 | 0.93508 | 0.86397 | 0.81335 | 0.69222 | 0.56149 | 0.45566 | 0.40571 | 0.33153 | 0.21158 | 0.16913 | 0.11144 | 0.091689 | 0.081688
Simulation results
Notes: I20Hz 0.610 0.565 0.696 0.692
R650°C 19.27 Ω 20.15 Ω 19.87 Ω 21.18 Ω

## Slide 15: Helping In Design
Same life time in simulation
Chart: Measurements with fabricated chip
| 1 | 3 | 5 | 7 | 10 | 13 | 15 | 20 | 27 | 35 | 40 | 50 | 80 | 100 | 150 | 180 | 200
Old Design | 1 | 0.99963 | 0.98569 | 0.94936 | 0.85831 | 0.7558 | 0.69371 | 0.56532 | 0.44187 | 0.35085 | 0.31006 | 0.25194 | 0.15825 | 0.12584 | 0.082932 | 0.068324 | 0.060942
New Design | 1.0172 | 1.0119 | 1.0029 | 0.98383 | 0.93508 | 0.86397 | 0.81335 | 0.69222 | 0.56149 | 0.45566 | 0.40571 | 0.33153 | 0.21158 | 0.16913 | 0.11144 | 0.091689 | 0.081688
Simulation results
Better than expected
Notes: I20Hz 0.610 0.565 0.696 0.692
R650°C 19.27 Ω 20.15 Ω 19.87 Ω 21.18 Ω

## Slide 16: Improve Design Process With Surrogate Modelling
3 geometrical parameters + applied electrical power
In parameter study only discrete combinations
Surrogate Modelling
Log(Ionic Flow)

## Slide 17: Improve Design Process With Surrogate Modelling
3 geometrical parameters + applied lectrical power
In parameter study only discrete combinations
Surrogate Modelling
Log(Ionic Flow)

## Slide 18: Application For Better Visualation
log(Ion Flux)

## Slide 19: Conclusion
Model building of existing technology without knowing exact material parameters
New evaluation of current designs
  Life time prediction
Developing new designs
  Better preselection of design worth manufacturing
  Surrogate Modelling allows steplessly adjustable parameters

## Slide 20: Thank you for your attention! Toni Schildhauer tschildhauer@cismst.de
QSolid
Funding code: 13N16172

## Slide 21: Verification experiment
Vacuum container
Source measure unit
Turbo pump
Remove influence of thermal conduction and convection by air
+
-
Unknown parameters:
Temperature dependent resistance
Temperature dependenent thermal conductivity
Notes: Temperaturmessung?

## Slide 22: Life Time Modeling
Dominant failure mechanism is Electromigration
K - summarized material properties, k - Boltzmann constant, T - Temperature, EA - Activation energy, E - Electric Field
+
-
E-Field of the IR-emitter
Analyzing current design
with perforated conductive layer
https://commons.wikimedia.org/wiki/File:Electromigration.png
Authour: Linear 77, Source: Own work