## Slide 1: Impact of Battery Operation and Manufacturing Process on Battery Performance over Lifetime
Thomas Bisgaard, Senior Simulation Specialist
André Gugele Steckel, Modelling Specialist
Martin Refslund Nielsen, Chief Commercial Officer, Robust Design Expert, and Partner

## Slide 2: Project Goals
Battery cell performance
Busbar/tab joint performance
System performance
& POSTER
PRESENTATION
Martin R. Nielsen
PRESENTATION
Andre G. Steckel
PRESENTATION
Design Tool

## Slide 3: Electrochemical Battery Model
Electrolyte (Li)/solvent
External circuit
Li+
Li+
Li+
e-
External circuit
e-
PF6-
PF6-
PF6-
Metal oxide particle
Li+
(Li)NiMnCoO2
Graphite particle
“Degradation” layer
Li+
Li
EC
EC
Li
Li
Cathode
Anode
Degradation
Li+
Lithium diffusion
Electric current distribution
Ionic current distribution
Intercalation
Anode
Separator
Cathode

## Slide 4: Electrochemical Battery Model
Anode particle
Solvent (EC)
Solvent diffusion through SEI layer
Reaction on particle surface
SEI Layer formation
Intercalation
Total
Mass balance in particle surface:
Degradation kinetics:
√ Loss of lithium inventory
√ Temperature
√ Current density
√ State-of-charge
Lithium:
Solvent:
Safari et al., Journal of The Electrochemical Society, 156 3 A145-A153 2009.
Li+
Spherical Electrode Particles
EC concentration at particle surface

## Slide 5: COMSOL Implementation
Electrochemistry & Degradation
Particle and SEI Layer Diffusion
Cathode
Anode
Separator
Cathode
Anode
Radial anode concentration
Radial Cathode concentration
Particle surface
Particle surface
Particle centre
Particle centre
Domain Mapping
1D
2D
Lithium mass balance
Current balance
Heat balance
Degradation
Lithium mass balance
Degradation

## Slide 6: COMSOL Implementation
Parameter set Sample generation
Python
SALib [1]
Model Builder
Application Builder
Simulation instance manager
Windows /COMSOL [3]
COMSOL Multiphysics
csv file
Experimental data
Battery Archive [2]
[1] https://salib.readthedocs.io/en/latest/ ; [2] www.batteryarchive.org; [3] COMSOL documentation
csv file
csv file
csv file
LHS Samples
Experimental Timeseries data
Stop Signal
Simulation Timeseries data
csv file
Cost Functions
Post processing
Python
SALib [1]
Analysis
COMSOL
Final simulation

## Slide 7: Parameter Fitting Method
Open cell voltage
Half cell voltage
SEM micrographs
Design /Manufacturer data
Fresh battery
Time-potential-current time series data
Charge /Discharge /Rest
Varying conditions (temperature, C-rates, SOC min /max)
Multiple cycling data
Time-potential-current time series data
Charge /Discharge /Rest
Varying conditions (temperature, C-rates, SOC min /max)
Pre-Cycling
Single Cycle (“Fresh”)
Multiple Cycles
1. Sample
2. Simulate
Acceptable ?
Yes
No
3. Evaluate
Uniform weight
First-principles parameters
System Parameters
Degradation
System parameters
Temperature dependent kinetics and diffusion
samples
datasets
Finish

## Slide 8: Expected vs Obtained Results
Cell Potential
[V]
Current
[A]
High current
2C/2C
Low current
0.2C/0.2C
High current
1.5C/0.2C
Low current
0.2C/0.2C
High current
1.5C/1.5C
Low current
0.2C/0.2C
Medium temp. 25°C
Low temp. -5°C
High temp. 45°C

## Slide 9: Expected vs Obtained Results

## Slide 10: Quality of Fit
Fresh Battery
Degradation
(samples)
(datasets)
(samples)
(datasets)
(cycles)

## Slide 11: Uncertainty and Sensitivity Analysis
Mechanical process tolerances Separator thickness variations
Cell Storage Conditioning variations Initial SEI layer thickness
Electrode process parameter limits Positive electrode particle radius
Inputs – Manufacturing Parameters
Outputs – Cell Quality Control
Battery Cell Electrochemical Model
Uncertain Parameter Sampling
Charge: 1C
Discharge conditions: Varying
Temperature: 25°C
[1] Sobol’, I.M., 2001. “Global sensitivity indices for nonlinear mathematical models and their Monte Carlo estimates”
Inputs – Operating Parameters
Load curve
Sensitivity Analysis
Sobol indices [1]:
Contribution to output variance
Overall effect
Uncertainty Analysis
Sample size=1024

## Slide 12: Uncertainty and Sensitivity Analysis
Variable | 1st cycle |  | 25th cycle | 
Potential |  |  |  | 
Histogram |  |  |  | 
Discharge energy 95% confidence interval [W*h] | 17.60 ≤ 17.75 ≤ 17.89 |  | 17.46 ≤ 17.71 ≤ 17.89 | 
Sensitivity [1] |  |  |  | 
 | 0.36 | 0.97 | 0.03 | 0.36
 | 0.38 | 0.86 | 0.30 | 0.78
 | 0.33 | 0.69 | 0.39 | 0.90
Variable | 1st cycle |  | 25th cycle | 
Potential |  |  |  | 
Histogram |  |  |  | 
Discharge energy 95% confidence interval [W*h] | 17.60 ≤ 17.75 ≤ 17.89 |  | 17.46 ≤ 17.71 ≤ 17.89 | 
Sensitivity [1] |  |  |  | 
 | 0.36 | 0.97 | 0.03 | 0.36
 | 0.38 | 0.86 | 0.30 | 0.78
 | 0.33 | 0.69 | 0.39 | 0.90
Ranking of variables for importance on output variance:
1 cycle: > >
25 cycles: > >
Optimization
Manufacturing cost example based on product specification:
Reduce by reducing variance on cathode particle size distribution.
[1] Sobol’, I.M., 2001. “Global sensitivity indices for nonlinear mathematical models and their Monte Carlo estimates”

## Slide 13: Conclusions
Successful implementation of an electrochemical model of a battery including degradation
Robust framework for parameter fitting
Parameters successfully tuned for data set (incl. temperature dependency)
Uncertainty/Sensitivity Analysis to quantify performance parameter variance
Uncertainty/Sensitivity Analysis to prioritize optimization efforts on e.g., manufacturing process
COMSOL Application Builder offers excellent freedom and flexibility for handling large data sets and complex scenario simulations

## Slide 14: Acknowledgement

## Slide 15: End of Presentation
Martin Refslund Nielsen
Commercial Lead, Partner
André Gugele Steckel
Modelling Specialist
Thomas Bisgaard
Simulation Specialist
Visit our website: https://resolvent.com/
Contact
Tel: +45 61 66 99 03 Email: info@resolvent.dk
Follow us on: https://www.linkedin.com/company/resolvent-p-s/