## Slide 1: Development of Quenching Process Recipe Using Simulation
J. KadkHodapour
Product Manager
andritz group
October 2024

## Slide 2: Insert chapter overview
01
Problem Statement
02
Data from Jmatpro
03
SimuLation by comsol
04
Result validation
05
Conclusion

## Slide 3: System Description
Simulation problem definition
1050ºC
450ºC
900ºC
780-250ºC
200ºC
500ºC

## Slide 4: System Description
Simulation problem definition

## Slide 7: Problem statement
Simulation problem definition: Data
Ref: US11890894B2 patent, 2019, Nippon Steel Corp
Distance from surface

## Slide 8: Hardness value in EN IRS-R-19/93 Standard
Test for measurement of hardness
The difference between extreme hardness values within a batch shall not exceed 30 BHN.
The microstructure of wheel shall be "Fine Pearlite structure with ASTM grain size 6 or finer."

## Slide 9: Insert chapter overview
01
Problem Statement
02
Data from Jmatpro
03
SimuLation by comsol
04
Result validation
05
Conclusion

## Slide 10: Simulation flow and required data
Standard Test for Hardenability
Jominy Test: based on ISO 642 is what we want to focus on and validate by simulations results

## Slide 11: Chemical compositions and Hardenability
Experimental Data for the 1045 Steel

## Slide 12: Chemical compositions and TTT Diagram
Experimental Data for the 1045 Steel and JMatPro output

## Slide 13: Insert chapter overview
01
Problem Statement
02
Data from Jmatpro
03
SimuLation by comsol
04
Result validation
05
Conclusion

## Slide 14: Comsol Simulation flow

## Slide 15: Model boundary conditions
Radiative Emisivity (ε) = 0.8
Heat Transfer Coefficient (hc) = *Next Slide
Dataloger

## Slide 16: Insert chapter overview
01
Problem Statement
02
Data from Jmatpro
03
SimuLation by comsol
04
Result validation
05
Conclusion

## Slide 17: Comsol simulation results

## Slide 18: Austenatizing temperature effect

## Slide 19: Martensite phase fraction
Martensitic microstructures for
Distance from quenched end: 1.6 mm.
Etching: Nital 3%.

## Slide 20: Bainite phase fraction
Microstructures for
Distance from quenched end: 4.8 mm.
Etching: Nital 3%.

## Slide 21: Pearlite phase fraction
Microstructures for
Distance from quenched end: 12.7 mm.
Etching: Nital 3%.

## Slide 22: Ferrite phase fraction
Microstructures for
Distance from quenched end: 12.7 mm.
Etching: Nital 3%.

## Slide 23: Insert chapter overview
01
Problem Statement
02
Data from Jmatpro
03
SimuLation by comsol
04
Result validation
05
Conclusion

## Slide 24: Conclusion
The combination of JMatPro and COMSOL can well predict the hardness of material after quenching.
Some further parametric study is required to be sure about the values of different phases from simulation.
The validated results can be used to design process for railway quench.

## Slide 25: Andritz Stays Hot On Your Trail To Uncover The Coolest Solutions!