## Slide 1
Stefano Caverni, Marco Lagnoni, Antonio Bertei
Advanced modelling for Li-ion battery design, diagnostics and R&D
Department of Civil and Industrial Engineering
University of Pisa - Italy

## Slide 2
Li-ion batteries in dynamic operations
Li-ion batteries are energy storage devices → no steady-state operation
We need to characterise dynamic processes: reactions, charge transport, diffusion, degradations, etc.
WLTC
Anode Cathode
GITT

## Slide 3
What hinders fast charging
Phase separation in Li-rich and Li-poor phases
Desired reaction: Li intercalation in graphite
Graphite
Electrons
Plated lithium
Intercalation
Li ions
Electrolyte
Intercalated lithium
Lithium plating
SEI
for E < 0 V vs Li
Undesired reaction: Li plating
*
Yang et al., Journal of Power Sources, 28-40,360, 2017
Stage 1L
*
Gao et al., Joule 5, 393–414, 2022

## Slide 4
What hinders fast charging
graphite
electrolyte
State of lithiation [-]
1 mm
Desired reaction: Li intercalation in graphite
Graphite
Electrons
Plated lithium
Intercalation
Li ions
Electrolyte
Intercalated lithium
Lithium plating
SEI
for E < 0 V vs Li
Undesired reaction: Li plating
*
Yang et al., Journal of Power Sources, 28-40,360, 2017

## Slide 5
Goals of the study
Model the interplay between graphite phase-separation and Li plating
Quantify kinetic and transport parameters
Develop model-guided fast-charging protocols

## Slide 6
graphite
electrolyte
State of lithiation [-]
1 mm
Electrochemical modelling: from 1D to 3D
Ion conservation
Electron and Li conservation
Phase-field approach
Kinetics of intercalation and plating
General Form PDE
+
Boundary ODEs
+

## Slide 7
Optical visualisation of intercalation and plating*
Li plating
Li metal loss
2 mA cm-2
100 mm
*X. Lu et al., Nat. Comm. 14 (2023) 5127

## Slide 8
Revealing the internal Li distribution
State of lithiation [-]
State of lithiation [-]
Model allows us to “look inside the particles” (radial distribution & diffusion limitations)
Model captures full evolution at all times:
  electrolyte transport
  phase separation
  lithium intercalation
  reversible plating
Strong validation of model and parameters

## Slide 9
Kinetics of Li intercalation and Li plating/stripping
Li intercalation occurs at phase boundaries
Plating takes place only on saturated graphite
Li plating is (partly) reversible
Back-intercalation at the phase boundary

## Slide 10
Lessons learned for model-guided charging protocols

## Slide 11
Take-home messages
Graphite phase separation and Li plating kinetics implemented in the model
Coupling with operando optical experiments for validation
Model-guided protocols enable fast-charging in 15 min
Non phase-separating anode materials (e.g., disordered carbon)

## Slide 12
Acknowledgments
These projects have received funding from :
Thank you!
The University of Pisa through the funding program “Progetti di Ricerca di Ateneo PRA 2020–2021”, project no. PRA_2020_48
“Network 4 Energy Sustainable Transition – NEST”, project funded under the National Recovery and Resilience Plan (NRRP), Mission 4 Component 2 Investment 1.3 – NextGenerationEU, project code PE0000021, Concession Decree No. 1561 of 11.10.2022 adopted by Ministero dell’Università e della Ricerca (MUR), CUP I53C22001450006 according to attachment E of Decree No. 1561/2022
“Integrated procedures for FAST ChARging with online state-of-health evaluation of lithium-ion batteries - FASTCAR ”, PRIN 2022, project funded by the Ministry of University and Research (MUR) under the National Recovery and Resilience Plan (NRRP), Mission 4 Component 2 Investment 1.3 – NextGenerationEU, CUP I53D23001550006
Prof. Antonio Bertei
Un. of Pisa
Dr. Xuekun Lu
Queen Mary Un. London
Students:
Andrea Distefano
Stefano Caverni